## Slide 1
1st International Conference
Earth Science And Energy
RESEARCH INNOVATION
IN MATERIALS SCIENCE
AND ENGINEERING
Prantasi Harmi Tjahjanti
UNIVERSITAS MUHAMMADIYAH SIDOARJO
Presented at: 1st International Conference Earth Science And Energy,
CitizenM Hotel, Bukit Tinggi, Kuala Lumpur, Malaysia
November 7-8 , 2019

## Slide 2: Outline
Introduction
Research Activity
Research of Drum Brake
Research Box Speaker of Mushroom Growing Media
Waste (MGMW)
Research of Graphene Oxide
Research of Alternative Materials for Ship Building

## Slide 3
MUDFLOW in Sidoarjo
13 Years Later 2006-2019
Introduction
Notes: Until now still issued a mudflow, even though the quantity is not large

## Slide 4
Univ. Muhammadiyah Sidoarjo

## Slide 5
Campus 1
5 Faculties:

## Slide 6
Campus 2
Campus 3

## Slide 7
Study Program
The undergraduate degree program in Mechanical Engineering
Faculty of Sience and Technology
Universitas Muhammadiyah Sidoarjo
RESEARCH FOCUS:
Energy Convertion
Manufacturing
Material & Metallurgy
Research Activity

## Slide 9
2003 – 2014:
Produksi Drum Brake Dari Material Komposit Berbasis Aluminum Untuk Komponen Otomotif Bersifat Ringan dan Memperlancar Transportasi Darat
Pembuatan Komponen Otomotif Brake Drum Dari Material Komposit Berbasis Aluminium Dengan Metode Centrifugal Casting Untuk Meningkatkan Faktor Efektivitas Rem
Analisa Korosi Pada Bahan Komposit Ber-Matrix Aluminium Dengan Reinforcement Bahan Keramik Silikon Karbida (SiC)
Pembuatan Plat Komposit Berbasis Aluminium Dengan Cara Pengecoran Sebagai Material Alternatif Untuk Bangunan Kapal
Pengaruh Coating Silikon Karbida (SiC) Terhadap Proses Pengecoran Aluminium Metal Matrix Cast Composite (AMMCC) Untuk Menunjang Efisiensi Bahan Industri Otomotif
Pengaruh Serabut Kelapa Sebagai Bahan Pengisi Komposit Bermatrik Polimer Termoset
Pengaruh Bahan Pengisi Caco3 Dan Al2o3 Terhadap Poliester Tak Jenuh Pada Pengujian Tarik
< 2003:
Sintesis dan Karakteristik Bahan Magnetik Nd15+xFe77-xB8 (x=0 ; x=3)
Studi Tentang Mikrostruktur dan Struktur Kristal Pada Pembentukan Superkonduktor (Bi-Pb)-2223 Melalui Prekursor (Bi-Pb)-2212
Pengaruh Variasi Dopan Pb pada Pembentukan Superkonduktor (Bi-Pb)-2223 Melalui Prekursor (Bi-Pb)-2212
Pengkajian Konduktivitas Listrik Bahan Campuran PE-CuO, PE-ZnO dan PE-Fe2
2015– 2022:
Keunggulan Dan Inovasi Pelapis Graphene – Polimer Sebagai Pelindung Korosi Baja ASTM A36
Pemodelan Dan Aplikasi Material Komposit EN AC-43100(AlSi10Mg(B))+SiC*/15p Untuk Struktur Kapal
Pengkajian, Pembuatan Dan Produksi Box Speaker Dari Material Komposit Berbasis Polimer Dengan Reinforcement Limbah Media Tanam Jamur

## Slide 10
Hasil penelitian Prantasi,dkk, dengan dana:
Penelitian Hibah Bersaing (2008 -2009) dan
-Penelitian Hibah Strategi Nasional (2012-2013-2014)
AlSi10 +SiC
DRUM BRAKE DARI MATERIAL KOMPOSIT BERBASIS ALUMINUM DENGAN PENGUAT SERBUK KERAMIK SiC (SILIKON KARBIDA)
Research of Drum Brake

## Slide 11
‘Lokasi’ drum brake di mobil
Figure 1. Drum brake serta tempat drum-nya
Figure 2. Bagian-bagian dari drum brake
Drum

## Slide 12
Gambar 3. Drum dibuka
Gambar 4. Drum <Drum Brake>

## Slide 13
Material drum brake:
Besi cor
Besi cor khusus
Baja cor
Harga besi dan baja merangkak naik (harga HRC (hot rolled coil)) mencapai sekitar US$600 per metrix ton
Densitas tinggi (7,9 gram/cm3),
jadi kendaraan secara keseluruhan
menjadi berat
Aluminium/
aluminium alloy
berat drum brake berkurang hingga
45–61% [Gerard,et.al 2000], kerena aluminium mempunyai densitas (2,7 gram/cm3) dan modulus elastisitas ± 1/3 dari besi
ketahanan ausnya berkurang [Scott Xiaodi Huang,et.al,1998], karena aluminium tergolong
bahan yang ‘lunak’ dibandingkan logam lainnya.
Secara keseluruhan mengurangi keunggulan sifat mekanis khususnya keefektivitasan rem pada otomotif tersebut.
Jadi: Penelitian ini penting untuk
mencoba membuat material
alternatif baru
Tidak tahan pada suhu tinggi (Tm≈7000C)

## Slide 14
Material alternatif baru dalam penelitian adalah:
Material Komposit Berbasis Aluminium
Dengan Cara Pembuatannya Menggunakan Teknik Pengecoran
(Aluminium Metal Matrix Cast Composite / AMMCC)
Keunggulan:
- Mempunyai sifat ringan, rendah biaya produksi,
berkualitas serta performance-nya tinggi secara
struktur.
- Lebih tahan terhadap temperatur tinggi karena
penurunan kekuatan yang dialami komposit berbasis
aluminium karena kenaikan temperatur, berlangsung
secara bertahap [Jerry GB,1998].
- memiliki kekuatan (strength) dan kekakuan spesifik
(specific stiffness) yang tinggi, koefisien muai panasnya
(Coeffisient of Thermal Expansion / CTE) rendah sekali
hampir mendekati nol.
- ketahanan ausnya cukup tinggi (high wear resistance),
ketahanan deformasi panasnya (rasio konduktivitas panas
terhadap koefisien muai panas) cukup baik, dapat
digunakan luas untuk bidang industri, karena dapat
diproses [WS Johnson,1987].

## Slide 15
Gambar. Mobil Jimny Katana tahun 1984

## Slide 16
Perhitungan dan gambar yang matang untuk drum brake dengan ANSYS

## Slide 17
Pencampuran antara SiC dengan Al murni pada suhu 600oC – 800oC, akan
muncul senyawa aluminium karbida (Al4C3), artinya terjadi reaksi kimia seperti persamaan di bawah ini:
4 Al(l) + 3 SiC(s)  Al4C3(s) + Si(s)
Aluminium karbida ini bersifat:
- Rapuh (brittle)
- Tidak dapat larut dalam aluminium yang telah cair.
- Membentuk lapisan kontinu maupun diskrit yang menyelubungi partikel SiC,
sehingga menyebabkan terjadinya retak antar muka (interface crack) antara
matrik Al murni dengan penguat SiC.
- Senyawa ini mempunyai formasi energi bebas yang terbentuk dari tiap mol
karbon dan lebih stabil secara termodinamika dibandingkan dengan SiC

## Slide 18
Casting Process

## Slide 19
257,5 mm
66,1mm
Hasil pengecoran  Drum brake dari material komposit matrik Al paduan dan penguat SiC

## Slide 20
Uji lapangan

## Slide 21
Uji Faktor Efektivitas Rem (FER)
di Dinas Perhubungan Kota Surabaya (UPTD Pengujian Kendaraan Bermotor Wiyung)

## Slide 22
Hasil Tahun Ketiga - Uji Produk
Mobil Avanza 2009 yang akan diganti drum brake-nya
Drum brake material komposit berbasis aluminum diperkuat dengan SiC yang telah dipasang di mobil Avanza 2009

## Slide 24
RESULT OF DRUM BRAKE THAT MAKE OF COMPOSITE MATERIAL BASED ON ALUMINUM AND SiC
The optimum of SiC is 15%
Value of heat conductivity is 14.42 W / (mK).
Wear resistant is 4,27 x 10-6 mm/mm3.
Hardness is 190,8 kgf/mm2
Energy to break 16,43 Joule.
Thermal expansion coefficient is 22.23 x 10-6/°C
Small rate of corrosion (Corrosion Penetration Rate / CPR) when coated of Cr-Ni and dipped in 0.1 M HCl solution for 6 hours, CPR obtained only 0.009.
Uji lapangan dilakukan dengan mengendarai mobil Jimny Katana 1984 dan mobil Avanza 2009 yang telah dipasang drum brake dari material komposit (Al-Si)+SiC/15%, menempuh jarak pulang-pergi Sidoarjo-Surabaya kurang lebih 60 – 70 km dengan kecepatan rata-rata 50 km/jam. Hasil yang terlihat bahwa drum brake tersebut tidak mengalami perubahan bentuk akibat panas maupun gesekan. Artinya secara keseluruhan drum brake ini dapat dipakai.

## Slide 25
Journal
IOP Conference Series: Materials Science and Engineering
Publication date: 2018/11
Volume: 434
Issue: 1
Pages: 012222
Publisher: IOP Publishing
doi:10.1088/1757-899X/434/1/012222
https://iopscience.iop.org/article/10.1088/1757-899X/434/1/012222/meta
Journal
Advanced Materials Research
Publication date: 2013/7
Volume: 789
doi:10.4028/www.scientific.net/AMR. 0.449
Pages: 449-454
Publisher: Trans Tech Publications, Switzerland
ISBN-13:978-3-03785-757-1
https://www.scientific.net/AMR.789.449
Published

## Slide 26
Numerical Modeling of Ship Composite-Based on Aluminum Casting as Alternative Materials for Ship Building
Matrix used is EN AC-43100 (AlSi10Mg (b) + SiC*/15p
European Nation = (EN)
Aluminum Casting = (AC)
using ANSYS version 12.0
1. Type and Sizes Ship
Fast Patrol Boat
Length over all (LOA) = 42,00 m
length between perpendiculars (LBP) = 39,00 m
Breadth (b) = 7,00 m
Height (H) = 4,00 m
Draft (T) = 1,8 m
Maximum speed = 24,0 knot,
Crew of ship = 18 person
Research of Alternative Materials for Ship Building

## Slide 27
Fig. 4 Distribution of stress in model of numerical for the full ship body for still water condition.
a. Aluminum ship EN AC-43100 (AlSi10Mg (b)) (maximum stress = 7.56 MPa).
b. Composite ship EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 7.24 MPa).
a
b
Fig. 5 Distribution of stress in model of numerical for the full ship body for wave induced
condition.
a. Aluminum ship EN AC-43100 (AlSi10Mg (b)) (maximum stress = 14.9 MPa).
b. Composite ship EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 14.1 MPa).
a
b

## Slide 28
Fig. 6 Distribution of stress in model of numerical for the hull and construction of
the base (bottom) for still wave condition
a. Ship aluminum EN AC-43100 (AlSi10Mg (b)) (maximum stress = 7.56 MPa).
b. Ship composite EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 7.24 MPa).
a
b
a
b
Fig. 7 Distribution of stress in model of numerical for the hull and construction of
the base (bottom) for wave induced condition
a. Ship aluminum EN AC-43100 (AlSi10Mg (b)) (maximum stress = 19.6 MPa).
b. Ship composite EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 19.1 MPa).

## Slide 29
Fig. 8 Distribution of stress in model of numerical for main deck for still water condition
a
b
a. Ship aluminum EN AC-43100 (AlSi10Mg (b)) (maximum stress = 7.16 MPa).
b. Ship composite EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 6.67 MPa
Fig. 9 Distribution of stress in model of numerical for main deck for wave induced condition
a
b
a. Ship aluminum EN AC-43100 (AlSi10Mg (b)) (maximum stress = 17.5 MPa).
b. Ship composite EN AC-43100 (AlSi10Mg (b))+SiC*/15p (maximum stress = 16.8 MPa)

## Slide 30
Table 4. Value of máximum stress of model of numerical
Distribusion stress | Composite material Aluminum material EN AC-43100 EN AC-43100 (AlSi10Mg(b))+SiC*/15p (AlSi10Mg(b) (thickness plate 6 mm) (thickness plate 6 mm)
 | Still Water Wave Induce Still Water Wave Induce (MPa) (MPa) (MPa) (MPa)
- Full body ship area 7.24 14.1 7.56 14.9 - Hull and construction of the base (bottom) area 7.24 19.1 7.56 19.6 - Main deck area 6.67 16.8 7.16 17.5 | 

## Slide 31
Application Analysis of Wall and Deck
Numerical of Modelling Composite Ship EN AC-AlSi10Mg (b)+SiC*/15p
By Using ANSYS ver. 12.0
Fig 2 Distribution stress of composite ship
EN AC 43100(AlSi10Mg(b))+SiC*/15p)
in superstructure wall with plate thick
5 mm (max. stress =9.43 MPa)
Fig 3 Distribution stress of composite ship
EN AC 43100(AlSi10Mg(b))+SiC*/15p)
on superstructure deck with plate thick
6 mm for induced wave condition
(max. stress = 10.7 MPa)

## Slide 32
The results of the stress distribution shows that:
Numerical modeling of ship aluminum AC-43100 EN (AlSi10Mg (b)) and composite ship EN AC-43100 (AlSi10Mg (b))+SiC*/15p) has successfully demonstrated the distribution stress to the full body ship, construction of the base (bottom), and main deck, for still water and wave conditions induced.
the maximum stress that occurs in induced wave conditions have higher value compared to still water conditions, because the load is included in the wave induced more numerous and complex than a given load on the still water.
Composite ship more weight than aluminum ship because in composite ship there have SiC as reinforcement, which causes the composite more heavier than the aluminum ship (for the same thickness = 6 mm).
Conversely, aluminum ship lighter, so it automatically receives the maximum stress is greater than that received by a composite ship, for input the same load and the plate of the same thickness.

## Slide 33
Journal: Advanced Materials Research
Publication date: 2013/7
Volume: 789
doi:10.4028/www.scientific.net/AMR. 0.143
Pages: 143-150
Publisher: Trans Tech Publications, Switzerland
ISBN-13:978-3-03785-757-1
https://www.scientific.net/AMR.789.143
Published
DOI: 10.2991/icaise.2013.46Conference: The International Conference on Artificial Intelligence and Software Engineering (ICAISE 2013)
Vol 11 No 6 (2019)
Publish: 2019-09-05
International Journal of Integrated Engineering (IJIE)
http://orcid.org/0000-0002-1655-3844
ISSN : 2229-838X
e-ISSN : 2600-7916

## Slide 34: Hasil penelitian Prantasi,dkk, dengan dana: PENELITIAN HIBAH KOMPETENSI (2015-2016-2017)

## Slide 35
Matrik I:
Unsaturated Polyster Resin (=> resin poliester)
Katalis: MEKPO=methyl ethyl ketone peroxides
Penguat/Reinforcement:
Ingredien of mushroom growing media :
-. sawdust -. bran -. calcium -. cornflour - white/red sugar -. gypsum (CaSO4) -. coconut water
- Organic fertilizer
-. water
baglog
-- dari desa Wonorejo Bumi Aji Kota Batu Malang, dari
Blitar, dan dari Sedati Sidoarjo
Perekat : Urea Formaldehyde cair
Limbah media tanam jamur (LMTJ)
Matrik II:
- MGMW
- Starch
- Urea
- PVC Glue
Research Box Speaker of Mushroom Growing Media
Waste (MGMW)
used for widen the slope of cliff area
(2014)

## Slide 36
mesin press menggunakan pemanas elpiji
mesin oven menggunakan mikrokontroler
Papan partikel komposit dari matrik resin poliester+katalis+LMTJ
Papan partikel komposit dari matrik kanji dan urea+lem PVC+LMTJ

## Slide 37
Standar Pemotongan Untuk Pengujian
Uji Fisis
Densitas(5x5cm)
Kadar Air (10x10cm)
Daya serap air (5x5cm)
Pengembangan Tebal
Uji Mekanis
MOR (5x20cm)
MOE
Internal Bond
8. Kuat pegang sekrup

## Slide 40
Box speaker dari Papan partikel komposit dari matrik resin poliester+katalis+LMTJ

## Slide 41
Box speaker dari Papan partikel komposit dari matrik kanji dan urea+lem PVC+LMTJ

## Slide 43
4. Composite particle board MGMW 60% + 1% + 39% PVC glue (50% starch + 50% urea) has a maximum value of the amplitude of vibration when compared to original speaker box.
5. Speaker box of composite particle board on mushroom growing media waste more good than original speaker box.

## Slide 44
Materials Science Forum
Vol. 966, pp. 210-214, 2019
August 2019
ISSN: 1662-9752
https://www.scientific.net/MSF.966.210
DOI:
https://doi.org/10.4028/www.scientific.net/MSF.966.210
Journal
AIP Conference Proceedings
Publication date: 2017/6/15, Volume: 1855, Issue: 1
Pages: 030014
Publisher: AIP Publishing
https://aip.scitation.org/doi/abs/10.1063/1.4985484
Published
Journal
IOP Conference Series: Materials Science and Engineering
Publication date: 2017/5, Volume: 196, Issue: 1, Pages: 012024
Publisher: IOP Publishing
Institute of Physics Publishing
https://iopscience.iop.org/article/10.1088/1757-899X/196/1/012024/meta

## Slide 45
The Analysis of Comparison CPR Between Coating Graphene Oxide+Waterborne Paint and Galvanized Coating in ASTM A36 Steel
Steel coating as long as including ASTM A36 steel is generally carried out by galvanizing or coating to provide corrosion resistance. However, the problems that occur with the commonly used layer will break and peel off when the steel is removed. The purpose of this study is to make of corrosion resistant steel coatings especially for ASTM A36 steel from a mix of graphene oxide + waterborne paint. Weight loss method for calculate Corrosion Penetration Rate (CPR). Corrosion testing by immersing ASTM A36 steel samples in seawater (NaCl), and corrosion test for room temperature and 5000C. Final results showed that CPR values ​​for ASTM A36 steel samples with graphene oxide (GO) + waterborne paint coating (WBp) obtained CPR value that did not exceeded the allowable standard rate (0.5 mm/yr). The microstructure of ASTM A36 steel that origin, coated with galvanizing and coated with graphene oxide + waterborne paint was observed using Scanning Electron Microscope (SEM) shows that the highest corrosion attact occurs in origin of ASTM A36 steel.
Research of Graphene Oxide
KEUNGGULAN DAN INOVASI PELAPIS GRAPHENE – POLIMER
SEBAGAI PELINDUNG KOROSI BAJA ASTM A36

## Slide 51
THANK YOU