## Slide 1
PRESENTED BY
Dr. Azad Kumar
Assistant Professor
Department of Chemistry
M.L.K. (P.G.) College, Balrampur
Photocatalytic degradation of Victoria blue dye in visible light by prepared TiO2/PPy/GO through oxidative polymerization
Human Resource Development Centre, Lucknow University, Lucknow

## Slide 2
Photocatalytic Reactions
Chemical reactions occurring in presence of semiconducting materials and light are known as photocatalytic reactions.
Semiconductors with suitable band gaps is a good quantum collectors of light energy.
Illuminating of desired energy photons on semiconductor material can cause a number of photocatalytic reactions.
Introduction
Photocatalysed Reaction
Wide spread applications in energy conversion
Pollution abatement
Synthesis of new materials
Fig.1: Photocatalytic Reaction

## Slide 3
Photocatalytic reactions :
(a) Homogenous Photocatalysis:-
In which photocatalyst (semiconductor) and substrate exist in the same phase
(b) Heterogeneous photocatalysis:-
Where photocatalyst and the substrate exist in different phases.
Types of semiconductors:
(a) n-type semiconductor:-
The n-type semiconductors are those, which exhibit conductivity due to the flow of majority electrons,
(b) p-type semiconductors :-
The p-type semiconductors exhibit conductivity due to the presence of positively charged majority holes.
Fig 2: Types of semiconductors

## Slide 4
Why is the need of photocatalyst ?
The dyes are responsible for the environmental contamination, due to the toxic properties.
The dyes are chemically stable and highly persistent in environment.
Lots of investigations has been reported that 10-12 % of dyes are used each year in synthesis in textile industries.
20% of dyes are lost during synthesis and processing operations, which enter into water through effluents.
The wastewater removed from industries contains highly hazardous and coloured pigments which causes serious impact on aquatic life and also human beings by producing carcinogenic effects.

## Slide 5
It has severe toxic effects on the human health.
The dyes are very dangerous when it comes to contact with skin and causes
Itchiness, Irritation, Reddening and Blistering.
It also affects to eyes like inflammation, eye redness, itching etc.

## Slide 6
There are several, physical and chemical methods have been studied to remove the organic dyes from the wastewater.
Coagulation, flocculation, reverse osmosis, , adsorption , adsorption on the activated, carbon, photosensitized oxidation, ion exchange method and ultra-filtration, have been used to reduce the toxic effects of dye effluents.
These are fairly effective only in removing pollutants, but main drawbacks involved in these techniques are transform of dyes into the secondary waste product which cannot treated again or dumped as such

## Slide 7
Titania (TiO2 ) used as photocatalyst
Band gap energy- 3.2 eV
Stable
Cheap
Non Toxic
Ecofreindly
Advantages of TiO2 using as photocatalyst
(a) High oxidative power, stability, and non-toxicity
(b) The process occurs under ambient conditions.
(c) The oxidation of the substrate to CO2 is complete in most cases and
(d) Inexpensive and remains quite stable in contact with different substrate.
Fig.3: TiO2 powder

## Slide 8
Large band gap of TiO2
Low quantum yield of TiO2
Low photon utilization efficiency,
Narrow spectrum of light, UV is the most responsive range
Separation of TiO2 from the treated water
Limitations of TiO2 using as photocatalyst
Band gap narrowing
Impurity energy levels
Oxygen vacancies
Charge separation
Methods of improvement of photocatalytic activity of Titania

## Slide 9
Band gap reduction
Doping with cations:
Ni, Fe, Co, Ag, Pt, Cr, Ba, Sr, Mn, Mg , Ag, Au, Pt, Pb and Pd etc are deposited on a TiO2 surface to enhance photocatalytic activity.
Doping with anions:
Anion-doped TiO2 photocatalysts, the mixing of the p states of the doped anion (N, S, F, Cl, O or C) with 2p states shifts of the oxygen, the valence band edge upwards, narrowing the band gap energy of TiO2
Nanocomposites:
coupled samples TiO2-CdS, Bi2S3-TiO2, TiO2-WO3, TiO2-SnO2, TiO2-MoO3 and TiO2-Fe2O3

## Slide 10
Applications of titania
Fig.5: Applications of TiO2

## Slide 11
Light
Source
Fig.7: Mechanism of photocatalysis and formation of electron hole pair
Mechanism of photocatalysis

## Slide 12
Excitation of electrons: Light absorption following excitation of electrons from the valence band of TiO2 to the conduction band to form electron/hole pairs.
Migration of hole/electron: Migration of electron/hole pairs thus formed to the TiO2 surface.
Initiation of redox reactions: Initiation of redox reactions to form active species such as hydroxyl radicals and superoxide ions
In some cases, intermediate products have been identified and reaction mechanisms have been proposed.
Steps of photocatalysis

## Slide 13
1- OH free radical theory
H2O + h+vb→ •OH + H+
•OH + dye → dye(ox)
2- The direct oxidation theory
h+vb + dye → dye(ox)
Different theories of photocatalysis

## Slide 14
Powder TiO2 fix with a binder
Inorganic binder is not influenced by photo-catalytic reaction.
The powder exposed on the surface can work effectively despite the total amount of powder contained in the binder.
We have to used the coating technology for photo-catalytic thin-film preparation that can cover all surface only with TiO2
Fig.8: Thin film photocatalysis on TiO2
Thin-film photocatalyst

## Slide 15
Effect of dye concentration
Size and structure of the photocatalyst
Effect of catalyst amount
Effect of pH
Surface area
Dissolve oxygen
Fig.9: Effect of surface area
Factors influencing the photocatalytic degradation

## Slide 16
Reaction temperature:
Temperature  Photodegradation
Inorganic ions:
Mg, Fe, Zn, Cu, BiCO3, phosphate, nitrate, sulfate and chloride
Effect of light intensity:
Light Intensity  Photodegradation
Effect of dopants on dye degradation:
Various transition metals, such as Ni2+, Zn2+, Cr3+ and Fe3+ can be easily incorporated into the crystal lattice of TiO2 because of their similar ionic radii (The ionic radii of Ni2+=0.72 Å, Zn2+=0.74 Å, Cr3+= 0.76 Å and Fe3+=0.69 Å are quite similar to that of host Ti4+=0.75 Å ions)
Factors influencing the photocatalytic degradation

## Slide 17
Presentation Topic
Photocatalytic degradation of Victoria blue dye in visible light by prepared TiO2/PPy/GO through oxidative polymerization

## Slide 18
Synthesis of polypyrrole
Synthesis of PPy/TiO2
Sonication for
30 min
Add H2SO4 (2.7 ml)
Stirrer 15 min
Pyrrole Solution+ Add.APS
(2.28 ml +50 ml H2O)
Stirring 4h
Dark green powder of PPy obtained
Dry in oven at 60oC
for 1 night
Dark green color soln.
Sonication for 30 min
Blue Solution+ add 1g TiO2
Stirrer for 15 min.
Filter and wash
Stirring 4h
Dark green color soln.
Dry in oven at 60oC
for 1 night
Filter and wash
Dark green powder of
PPy/TiO2 obtained
Synthesis of PPy and PPy/TiO2
Blue solution.
1.727 ml pyrrole +50 ml H2O mix.
Soln.of Ppy/ TiO2+ APS (4.56 ml + 100 ml H2O)
3.45 ml pyrrole+100 ml H2O
+ 5.43 ml H2SO4 mix

## Slide 19
3.45 ml pyrrole + 100 ml H2O + 5.43 ml H2SO4 mix
Sonication for 30 min
Blue Solution+ added 1g TiO2
Stirrer for 15 min.
Soln. of PPy/ TiO2+ APS soln.+ 60 mg graphene oxide mix.
Add from burrate for 30 min.
Dark green color soln.
Dry in oven at 60oC for 1 night
Filter and wash
Dark green powder of PPy/TiO2/GO obtained
Synthesis of PPy/TiO2/GO

## Slide 20
Fig.67: X-Ray diffraction of
(a) TiO2
(b) Pure PPy
(c) TiO2/PPy (d)TiO2/PPy/GO
Sample Particle Size
TiO2 19 TiO2/PPy 24 TiO2/PPy/GO 30
Table 9: Average size of particles/grains in the samples of TiO2, TiO2/PPy, TiO2/PPy/GO
Results

## Slide 21
Fig.68: TEM of (a) TiO2 (b) Pure PPy (c) TiO2/PPy (d) TiO2/PPy/GO
TEM images

## Slide 22
Fig.69: SEM images of (a) pure PPy, (b) pure TiO2, (c) TiO2/PPy (d) TiO2/PPy/GO nanocomposites.
SEM images

## Slide 23
Fig.70: FTIR spectra of TiO2, PPy, TiO2/PPy and TiO2/PPy/GO
FTIR Spectra
Peak at 1554 and 1474 cm−1 are due to the fundamental vibrations of polypyrrole ring,
Peak at 1294 and 1049 cm−1 are due to the = C–H in-plane vibrations
Peak at 1196 cm−1 is due to the C–N stretching vibrations.
Structure of PPy

## Slide 24
Fig.71: UV-Vis spectra of (a) pure TiO2, (b) TiO2/PPy (c) pure polypyrrole (d) TiO2/PPy/GO nanocomposites.
UV-Vis spectra

## Slide 25
Fig.72: Band Gap energy of (a) pure TiO2 (b) pure PPy (c) TiO2/PPy (d) TiO2/PPy/GO nanocomposites.
Eg value
TiO2 :- 3.2
PPy :-2.4
TiO2/PPy:- 2.9 TiO2/PPy/GO:- 2.6
Band gap energy (Eg)

## Slide 26
The % degradation efficiency of dye was calculated by Equation (2).
Where  is the degradation efficiency, Ao is the initial absorbance and AF is the final absorbance
Photodegradation of dyes

## Slide 27
Fig. 73: Effect of concentration on photodegradation efficiency of dyes Victoria blue
Photodegradation of dyes
Effect of concentration
Effect of pH
Fig. 74: Effect of pH on photodegradation efficiency of dyes Victoria blue

## Slide 28
Fig.75. Effect of photocatalyst amount on efficiency of dyes Victoria blue
Photodegradation of dyes
Effect of photocatalyst amount
Effect of Irradiation Time
Fig. 76: Effect of irradiation time on photodegradation efficiency of dyes Victoria blue

## Slide 29
Fig.77: Photodegradation of Victoria Blue and Rose Bengal by Photocatalyst and recyclable Photocatalyst (a) TiO2 (b) Recycled TiO2 (c) TiO2/PPy (d) Recycled TiO2/PPy (e) TiO2/PPy/GO (f) RecycledTiO2/PPy/GO
Recyclability of Photocatalyst
The photodegradation of dye is decreasing slightly with recycled nanocomposites.
This is due to the lost of some active sites in the photocatalyst

## Slide 30
Fig.78: Photolumiscence Spectra of TiO2, TiO2/PPy and TiO2/PPy/GO
Fig.79: PL spectra of photocatalyst with terephthalic acid (0.001M) TiO2, TiO2/PPy and TiO2/PPy/GO
Lowering of electron-hole recombination
Mechanism of photocatalysis
Hydroxyl radical formation

## Slide 31
Fig.79: Mechanism of Photodegradation by Ti O2 encapsulated PPy
Mechanism of photocatalysis

## Slide 32
Fig.80: Linear first order reaction of Langmuir Hinshelwood kinetics of Victoria Blue (a) TiO2 (b) TiO2/PPy (c) TiO2/PPy/GO
Kinetics of photodegradation
Photodegradation of dyes follows the First order kinetics

## Slide 33
In this research work describes a proficient method for synthesis of TiO2/PPy and TiO2/PPy/GO nanocomposites.
These nanocomposites were prepared by one-step in situ deposition oxidative polymerization of pyrrole.
Ammonium per sulphate (APS) used as an oxidant in the presence of TiO2 nanoparticles cooled in an ice bath.
The obtained nanocomposites were characterized by XRD, TEM, SEM, UV-Vis, FTIR, techniques.
The obtained results showed that TiO2 nanoparticles have been encapsulated by PPy with a strong effect on the morphology of TiO2/PPy and TiO2/PPy/GO nanocomposites.
Conclusion

## Slide 34
The Photocatalytic degradation of Victoria blue dye was done at different condition viz concentration of dye, time of illumination, pH and dose of photocatalyst.
The maximum photodegradation were found at 7 pH, 20 ppm concentration of Victoria blue solution, 800 mg/L amount of photocatalyst and 120 min irradiation of visible light for VB .
Kinetics of photodegradation was investigated for Victoria blue dye and found first order kinetics.
The coating of PPy and GO were enhanced the photocatalytic activity of Titania.
Hence TiO2/PPy and TiO2/PPy/GO are the efficient photocatalyst for the degradation of Victoria Blue dye than pure TiO2.
Conclusion

## Slide 35
Thank You
for
YOUR
Kind
Attention