## Slide 1: Effect on electrospun fibers by synthesis of high branching poly-lactic (PLA)

## Slide 2: Introduction
In this study, we synthesized high branching PLA. We characterized the ultra-high molecular weight hydrophilic high branching polylactic acid by IR, 1H-NMR, GPC and DSC. In addition, from the different surface morphology of films characterized by atomic force microscope (AFM), it is found that high branching PLA has higher pores forming ability, and its porous nanofibers were prepared by electrospinning of phase separation solution. The adsorption of silver ion (Ag+) results showed that porous nanofibers of the high branching PLA had a high adsorption of Ag+. The high branching PLA has a potential possibility as scaffold for tissue engineering or antibacterial dressing.

## Slide 3: Chemical formula of the highly branched PLA

## Slide 4: FTIR spectrum of linear PLA

## Slide 5: FTIR spectrum of 3-arm PLA

## Slide 6: FTIR spectrum of high branching PLA

## Slide 7: 1H-NMR spectrum of linear PLA

## Slide 8: 1H-NMR spectrum of 3-arm PLA

## Slide 9: 1H-NMR spectrum of high branching PLA

## Slide 10: DSC curves about the first heating scan of linear PLA

## Slide 11: DSC curves about the first heating scan of 3-arm PLA

## Slide 12: DSC curves about the first heating scan of high-branching PLA

## Slide 13: DSC curves about the second heating scan of linear PLA

## Slide 14: DSC curves about the second heating scan of 3-arm PLA

## Slide 15: DSC curves about the second heating scan of high branching PLA

## Slide 16: GPC characterization results
 | level | Mw | Mw Error | PDI | PDI Error
Sn(Oct)2 W% | 1.5% | 75136 | 10633 | 3.699 | 0.453
 | 2% | 19726 | 9102 | 1.687 | 0.21
 | 2.5% | 167306 | 22798 | 1.586 | 0.166
 | 3% | 69761 | 6467 | 1.208 | 0.171
 | 3.5% | 5603 | 3236 | 1.564 | 0.122
Time | 8h | 167306 | 22798 | 1.586 | 0.166
 | 16h | 223047 | 57412 | 1.479 | 0.102
 | 24h | 743951 | 70900 | 1.218 | 0.071
 | 32h | 638651 | 96128 | 1.398 | 0.126
 | 40h | 642187 | 74937 | 1.187 | 0.057
Reactant ratio (glycerol: Lactide / mol:mol) | 1:100 | 743951 | 70900 | 1.218 | 0.071
 | 1.5:100 | 1.02E+06 | 126408 | 1.637 | 0.277
 | 2:100 | 657105 | 75967 | 1.197 | 0.097
 | 2.5:100 | 543218 | 39584 | 1.52 | 0.226
 | 3:100 | 107586 | 64330 | 2.388 | 0.31

## Slide 17: GPC characterization of branching PLA with molecular weight of 1,000,000 Da

## Slide 18: Surface features of linear PLA, 3-arm PLA and high branching PLA obtained by AFM
Linear PLA
3-arm PLA
High branching PLA

## Slide 19: Morphology of linear PLA electrospun fibers obtained at different temperatures
Electrospun fibers were carried out in spinning chamber at a relative humidity of 35% from 20 °C - 40 °C, voltage was 15kV, the electric distance was 10cm, the injection speed was 1.2 ml/h, the syringe needle was No. 6 with flat-ended.
20 °C
30 °C
40 °C

## Slide 20: Morphology of 3-arm PLA electrospun fibers obtained at different temperatures
Electrospun fibers were carried out in spinning chamber at a relative humidity of 35% from 20 °C - 40 °C, voltage was 15kV, the electric distance was 10cm, the injection speed was 1.2 ml/h, the syringe needle was No. 6 with flat-ended.
20 °C
30 °C
40 °C

## Slide 21: Morphology of high branching PLA electrospun fibers obtained at different temperatures
Electrospun fibers were carried out in spinning chamber at a relative humidity of 35% from 20 °C - 40 °C, voltage was 15kV, the electric distance was 10cm, the injection speed was 1.2 ml/h, the syringe needle was No. 6 with flat-ended.
20 °C
30 °C
40 °C

## Slide 22: Morphology of electrospun fibers obtained at humidity of 45%, 40°C, 15kV
Morphology of linear PLA(a), 3-arm PLA (b)and high branching PLA(c) electrospun fibers obtained at humidity of 45%, 40°C, 15kV
a. linear PLA
b. 3-arm PLA
c. high branching PLA

## Slide 23: Morphology of electrospun fibers obtained at humidity of 45%, 40°C, 18kV
Morphology of linear PLA(a), 3-arm PLA (b)and high branching PLA(c) electrospun fibers obtained at humidity of 45%, 40°C, 18kV
a. linear PLA
b. 3-arm PLA
c. high branching PLA

## Slide 24: Surface features by OCA
Surface features of linear PLA (a), 3-arm PLA (b) and high branching PLA(c) obtained by OCA.
a. linear PLA
b. 3-arm PLA
c. high branching PLA

## Slide 25: Surface features of electrospun fibres by OCA
a. linear PLA
b. 3-arm PLA
c. high branching PLA
OAC of linear PLA (a), 3-arm PLA (b) and high branching PLA (c) electrospun fibres obtained at humidity of 45%, 40℃, 18 kV.

## Slide 26: Adsorption of Ag+ by different fibers Wide spectrum and Ag peak of linear PLA fiber
Fibers prepared by 5ml electrospun solution at 40 °C were used for this experiment. The porous fibers were added into AgNO3 solution of 0.5 g/100 mL for 20 min to adsorb Ag+, which were dried at 30 °C.

## Slide 27: Adsorption of Ag+ by different fibers Wide spectrum and Ag peak of 3-arm PLA fiber
Fibers prepared by 5ml electrospun solution at 40 °C were used for this experiment. The porous fibers were added into AgNO3 solution of 0.5 g/100 mL for 20 min to adsorb Ag+, which were dried at 30 °C.

## Slide 28: Adsorption of Ag+ by different fibers Wide spectrum and Ag peak of high branching PLA fiber
Fibers prepared by 5ml electrospun solution at 40 °C were used for this experiment. The porous fibers were added into AgNO3 solution of 0.5 g/100 mL for 20 min to adsorb Ag+, which were dried at 30 °C.