## Slide 1: X-ray Absorption Spectra Prediction of Extended Graphene Oxide Nanoflakes using Graph Neural Networks
Samuel J. Hall1, Kanishka Singh1,2, Qinyuan Zhou1,2 and Annika Bande1,3
RACXS
12th June 2024
Helmholtz-Zentrum Berlin für Materialien und Energie GmbH, Berlin, Germany ​
Institute of Chemistry and Biochemistry, Freie Universität Berlin, Berlin, Germany
Leibniz Universität Hannover, Hannover, Germany

## Slide 2: Graphene Oxide (GO) Nanoflakes
GO have promising uses in photocatalyst, nanoelectronics, batteries and anti-corrosion coatings. [1,2]
Problems to experimentally characterise, large nanoflakes, irregular structure
Possible to represent as smaller more manageable molecules [3]
n
Notes: GO nanoflakes are too large to compute
We can reduce and represent as smaller molecules
Create a database of various molecules with a collection of oxidised groups

## Slide 3: GO Dataset
Database of 317 coronene molecules with a random collection of oxidation groups.
  1030 epoxide 437 Alcohol 172 carboxylic acid 159 ketone 117 aldehyde
Carbon XAS were calculated for every carbon atom – 7895 spectra.
XAS calculated using TDDFT with the ORCA package
  BH0.57LYP functional
  def2-TZVP basis set
  Gaussian broadening applied to spectra
Notes: More information about the dataset
317 molecules, 7895 atoms, x, y, z functional groups
ORCA TDDFT

## Slide 4: Predicting XAS Spectra
Graph neural networks (GNNs) have been successfully used to predict XAS. [1-3]
To test the prediction of larger structures, test set of 91 circumcoronene molecules was created
?
Notes: Goal is to create a ML model from the dataset to predict XAS
How can we use the model to predict XAS of larger systems like nanoflakes
To look at this created a test set of 91 circumcoronene molecules

## Slide 5: Graph Neural Networks (GNNs)
All molecules were represented as graphs.
Node and edge feature vectors represent atom and bond properties.
Node Features | Edge Features
Atomic number | Single bond
Degree | Double bond
Number of Hs | Aromatic bond
Number of Os | Conjugated
Hybridization | In ring
Aromatic | 
Represented as one-hot encoding
Notes: Details of the ML model
Feature vectors of nodes and bonds
Hyperparameters of model
RSE equation

## Slide 6: ML Model
15
64
200
128
256
256
Input
Convolutional Layers
GCN
Mean
Pool
Output
256
Linear Layer
Layer Length
ML hyperparameters
ReLU activation
Dropout = 0.5
Learning rate = 0.01
Adam optimizer
85:15 split
300 epochs
Accuracy of predicted and “true” spectra calculated through relative spectral error (zero means no difference).
Information propagates through graph
GCN Layers
3
1
4
2
5
6
7
8
6
5
7
3
2
1
4
5
5
8
GCN
GCN
GCN
GCN
5
Notes: Details of the ML model
Feature vectors of nodes and bonds
Hyperparameters of model
RSE equation

## Slide 7: Molecule PredictionResults
For a rather small dataset, the XAS of the whole molecule can give accurate predictions.
Results show using graph convolutional layers.
Notes: Initial test on whole molecules
Performance good for a limited dataset size
The choice of gnn layer doesn’t really change performance, all are very similar

## Slide 8: Predicting Larger Systems
Overall performance of the larger circumcoronene molecules comparative to coronene.
Coronene
Circumcoronene
Notes: How does the model fair when dealing with larger systems
Looking at the differences model types there is a slight improvement with graphsage

## Slide 9: Atom XAS Prediction
Node/atom spectra prediction offers a more localized prediction.
Combine graph embedding with individual node embedding.
15
64
200
128
256
256
Input
GCN Layers
Mean
Pool
Output
256
Linear Layer
Layer Length
+
+
+
+
+
Node
Vector
+
Notes: A more ideal method would be to predict the individual atom spectra
Describe the difference with the pooling

## Slide 10: Atom XAS Prediction
Performance on node/atom XAS prediction an order of magnitude worse – molecule prediction RSE ≈ 0.035.
Average RSE prediction
Model can generally predict main XAS features.
Problems arise from shifts between similar environments.
Notes: A more ideal method would be to predict the individual atom spectra
Describe the difference with the pooling

## Slide 11: Summary and Outlook
Possible to predict XAS of larger structures from datasets of smaller ones.
  Results are only for small dataset size
  Not larger extended systems
?
Aim to predict atomic XAS.
  Overall performance not as good.
  Issues with shifts from geometry (bond length, geometry)
  GAT, GINE, GraphSAGE
Notes: Predicting spectra of larger systems would be very useful
Models loose performance when dealing with molecule representation
Atom spectra prediction would be a better method

## Slide 12: Thank you for your attention!
Any questions?