## Slide 1: Data-driven capture and analysis of core-level spectra
Recent Advances in Computer-aided X-ray Spectroscopy
Samantha Tetef, Yiming Chen, Haili Jia, Davis Unruh, Chaitanya Kolluru, Zisheng Zhang, Joydeep Munshi, Eric Schwenker, Trevor Spreadbury, Weixin Jiang, Arun Baskaran, Arun Mannodi-Kannakithodi, Justin Pothoof, Spencer Hills, Liang Li, Fatih Sen, Maria Chan
Center for Nanoscale Materials
Argonne National Laboratory

## Slide 2: Collaborators
4DSTEM
Colin Ophus (LBL)
Alex Rakowski (LBL)
Shreyas Cholia (LBL)
TEM/STEM
Xiaobing Hu (Northwestern)
Vinayak Dravid (Northwestern)
Jinglong Guo (UIC)
Robert Klie (UIC)
Peter Crozier (ASU)
Paul Voyles (UW-Madison)
STM
Rui Zhang (ANL)
Jeff Guest (ANL)
Qiucheng Li (Northwestern)
Mark Hersam (Northwestern)
Literature data
Gerbrand Ceder (LBL)
Amalie Trewartha (LBL)
VISIMO
XAS/XES/EELS
Jerry Seidler (UW)
Ajith Pattammattel/Yong Chu (BNL)
Inhui Hwang/Chengjun Sun (ANL)
Eli Stavitski (BNL) Deyu Lu (BNL)
Xiaohui Qu (BNL)
Wanli Yang (LBL)
Shyue Ping Ong (UCSD)
Chi Chen (Microsoft)
Mariana Bertoni (Arizona State)
Srisuda Rojsatien (Arizona State)
Eric Shirley (NIST)
John Vinson (NIST)
Yuzi Liu (ANL)
Steve Heald (ANL)
XRD
Brian Toby (ANL)
Bob von Dreele (ANL)
Force fields/Digital Twins
Subramanian Sankaranarayanan (ANL)
Stephen Gray (ANL)
Mathew Cherukara (ANL)
Bobby Sumpter (ORNL)
Jan-Michel Carrillo (ORNL)
Haidan Wan (ANL)
Data Science/Computer Vision
Michael Davis (ANL)
Ben Blaiszik (UChicago)
Nicola Ferrier (ANL)
Ollie Cossairt (Northwestern)

## Slide 3: Focus: Nanoscale structures for energy materials
Batteries
Xiang Liu, Gui-Liang Xu, Chaitanya Kolluru et al, “Origin and regulation of oxygen redox instability in high-voltage battery cathodes”, Nature Energy (2022).
Catalysis
L. Chong, J. Kubal, F. Sen et al, “Ultralow-loading platinum-cobalt fuel cell catalysts derived from imidazolate frameworks,” Science (2018).
Photovoltaics
J Guo et al, “Effect of selenium and chlorine copassivation in polycrystalline CdSeTe devices,” Applied Physics Letters (2019).

## Slide 4
Experimental
Characterization data
Oxygen
Transition metal
Lithium
Data Driven
Theory
Animation: Johnson Matthey Technol. Rev., 2015, DOI: 10.1595/205651315x685445

## Slide 5
Theory
Experimental Spectroscopy Data
Oxygen
Transition metal
Lithium
Animation: Johnson Matthey Technol. Rev., 2015, DOI: 10.1595/205651315x685445

## Slide 6
Li
O
Fe
cation disordering
-2 Li
Li3FeO3.5
cation-disordered
Li5FeO4
anti-fluoride
Li6-O
What is the coordination of oxygen in Li5-xFeO4?
C. Zhan, et al, “Enabling the high capacity of lithium-rich anti-fluorite lithium iron oxide by simultaneous anionic and cationic redox,” Nature Energy 2, 963–971 (2017).
Zhenpeng Yao et al, "Exploring the Origin of Anionic Redox Activity in Super Li-Rich Iron Oxide-Based High-Energy-Density Cathode Materials." Chemistry of Materials (2022).

## Slide 7: Oxygen Local Environments in Li3FeO3.5
Li
O
Fe
AIMD at 15 ps
AIMD at 20 ps
NFe = 0
NFe = 1
NFe = 2
NFe = 3
NFe = 4
Fe coordination is an indicator of oxygen electronic structure and capacity due to oxygen activity.
cutoff radius = 2.6 Å

## Slide 8: Simulated O K-edge XANES
Simulations of original Li5FeO4 matches experiments of pre-cycled material
Upon charging to Li3FeO3.5, spectra from structures with peroxo/superoxo match better
Is this pre-edge feature from O-O?

## Slide 9: Simulated O K-edge XANES
Li3FeO3.5
with peroxo O-O dimer
with superoxo O-O dimer
L. Li, E.J. Lee, J. Freeland, T. Fister, M. Thackeray. M.K. Y. Chan, J. Phys. Chem. Lett., 10, 806 (2019)
Decomposing spectra from different types of oxygen shows it’s actually Li6O units, not O-O, that give rise to pre-edge feature

## Slide 10
Experimental Spectroscopy Data
Oxygen
Transition metal
Lithium
Data Driven
Animation: Johnson Matthey Technol. Rev., 2015, DOI: 10.1595/205651315x685445

## Slide 11: XANES mapping – materials are messy
Wang et al, “In situ chemical mapping of a lithium-ion battery using full-field hard X-ray spectroscopic imaging”, 10.1039/C3CC42667J
https://www.nanoscience.com
Inhomogeneous lithiation

## Slide 12: Analysis of XANES mapping data is demanding
A. Pattammattel, Sci. Adv., 6, eabb3615 (2020)
Each pixel is 150 nm wide and is one XANES spectrum.
There are ~25,000 spectra in this image.
Latest advancements:
Improved photon brilliance
Full-field imaging detectors / faster monochromators
How to extract phase information from data?

## Slide 13: Linear combination fitting (LCF) XANES analysis
Nano-XANES: every pixel (150 nm) has an associated XANES spectrum
… in this case Fe K-edge XANES
Stainless Steel
Fe3P
Pyrite
LiFe(II)PO4
Magnetite
Fe(III)SO4
Fe(III)PO4
Hematite
Maghemite
Goethite
HFO
Possible phases form
a reference library
Get phases from references
What can go wrong here?

## Slide 14: Problem 1: Identifying phases depends on LCF results
Problem:
Reference spectra can be highly correlated
Instead, we flip the order, identifying similar regions in the image (image segmentation) and then perform LCF on the averages.
Problem:
Pixel-by-pixel analysis can cause unphysical fluctuations
The usual procedure is to take the XANES spectrum at every pixel and independently perform linear combination fitting (LCF) onto a reference library.

## Slide 16
6 principal components explain 97% of the variance of all spectra in the XANES map
S. Tetef et al, “Manifold Projection Image Segmentation for Nano-XANES Imaging,” APL Machine Learning 1, 046119 (2023)

## Slide 17
Instead of simply including the spectra at each pixel, we embed
Principal components of spectra (6)
X-ray florescence signals of several elements
Spatial location (x, y)
a and b are tuning parameters to determine the weight between the 3 different inputs
S. Tetef et al, “Manifold Projection Image Segmentation for Nano-XANES Imaging,” APL Machine Learning 1, 046119 (2023)

## Slide 18
S. Tetef et al, “Manifold Projection Image Segmentation for Nano-XANES Imaging,” APL Machine Learning 1, 046119 (2023)
UMAP+dbscan provide cleaner clusters than PC+kmeans

## Slide 19
Question:
How does MPIS (without auxiliary XRF data) compare to the standard analysis procedure when there is a lot of noise in the experiment?
Answer:
The identification of clusters remains the same, so MPIS is more robust.
S. Tetef et al, “Manifold Projection Image Segmentation for Nano-XANES Imaging,” APL Machine Learning 1, 046119 (2023)

## Slide 20
Question:
How does incorporating auxiliary XRF data into the algorithm help?
Answer:
The auxiliary XRF data helps recover the lost phase when noise is large.
S. Tetef et al, “Manifold Projection Image Segmentation for Nano-XANES Imaging,” APL Machine Learning 1, 046119 (2023)

## Slide 21: Problem 2: Imaging takes forever
Instead of sacrificing spatial points, we will take fewer energy measurements to achieve full spatial maps.
This image has 24,800 XANES spectra.
… in this case Fe K-edge XANES
Intelligent spatial sampling
Identifying Regions of Interest (ROIs) via XRF
Strategies for reducing the required number of XANES spectra:
S. Tetef et al, “Accelerating nano-XANES imaging via feature selection,” Digital Discovery 3, 201 (2024).

## Slide 22: How to ensure robustness with fewer energies?
Thus, we will utilize our highly robust analysis procedure, which can handle the fewer energy spectra. We will determine the best energies to measure using feature selection.
Fewer energies means less data, which might decrease the accuracy and increase uncertainties in analysis results.
To tackle the fact that imaging takes forever, we want to intelligently sample energies.
S. Tetef et al, “Accelerating nano-XANES imaging via feature selection,” Digital Discovery 3, 201 (2024).

## Slide 23: Recursive feature elimination to choose energies
S. Tetef et al, “Accelerating nano-XANES imaging via feature selection,” Digital Discovery 3, 201 (2024).
~16 energy points would be sufficient

## Slide 24: Spectra & phases are well reconstructed with the subset of 16 energies.
S. Tetef et al, “Accelerating nano-XANES imaging via feature selection,” Digital Discovery 3, 201 (2024).

## Slide 25
Theory
Experimental Spectroscopy Data
Oxygen
Transition metal
Lithium
Data Driven
Animation: Johnson Matthey Technol. Rev., 2015, DOI: 10.1595/205651315x685445

## Slide 26: Advanced, multimodal, operando/in-situ characterization increasingly used
???
X-ray
Electron
Atom
Laser
etc
How do we invert characterization data to get atomic structures?
Notes: In order to deduce properties of battery interfaces, structures are critical. But at interfaces, there are often a large number of possible structures with similar energies. One important aspect of our work is the use of both characterization data and atomistic modeling to produce three-dimensional structures.

## Slide 27: Forward simulations
Core level spectra - Accuracy
https://github.com/MaterialEyes/atomagined
Electron microscopy
– realistic noise
Raman spectra – speed
Liang Li, Eric Schwenker, Nina Andrejevic

## Slide 28: Benchmark for Ni XANES references
FEFF and VASP perform similarly in terms of Pearson correlation
Ni K-edge spectra are simulated using VASP
Using Pearson correlation to quantify similarity
Fixed energy range for all spectra
Yiming Chen

## Slide 29: Variance among experimental data
[1] You, Bo, et al. Chemistry of Materials 27.22 (2015): 7636-7642.
[2] Sa, Young Jin, et al. ACS Catalysis 9.1 (2018): 83-97.
[3] Zheng, Xusheng, et al. Journal of Physics: Conference Series. Vol. 430. No. 1. IOP Publishing, 2013.
[4] Chen, Liliang, et al. Nanotechnology 24.4 (2013): 045602.
[5] Chou, Shih-Cheng, et al. Materials 13.12 (2020): 2703.
[6] Jia, Mingwen, et al. Chemical science 9.47 (2018): 8775-8780.
[7] Wang, Dewen, et al. ACS central science 4.1 (2018): 112-119.
[8] Xu, Yingqi, et al. Frontiers in Materials 6 (2019): 271.
[9] Yan, Binhang, et al. Proceedings of the National Academy of Sciences 115.33 (2018): 8278-8283.
The Pearson correlation within experimental data is around 0.99
0.993-1.000
0.979-0.997
0.999
0.995-0.999
Yiming Chen

## Slide 30: Pretrained model – core-level spectroscopy How to represent spectra?
Featurization: turning input data into a “better” form for machine learning
?
3000 Ni K-edge simulated with VASP

## Slide 31: Featurization + ML workflow
Yiming Chen et al, “Robust Machine Learning Inference from X‑ray Absorption Near
Edge Spectra through Featurization,” Chemistry of Materials 36, 2304 (2024)

## Slide 32: Featurization approaches
Intensity ([1, 100])
Cumulative distribution function ([1, 100])
Peak feature ([1,60])
  Decompose the spectroscopy into addition of 20 gaussian peaks
Continuous wavelet transform ([10,100])
  An overcomplete representation of signal by varying the parameters of wavelets, common to EXAFS analysis
Yiming Chen, Michael Davis, Chi Chen, Shyue Ping Ong

## Slide 33: Test system: Li(Ni,Mn,Co)O2 battery materials
Generated ~2800 Ni K-edge XANES spectra for 700 NMC structures including different NMC compositions and Li contents.
Average bond length (Å)
Oxygen
Ni, Mn, Co
Lithium
Notes: explicitly state that the spectra are not clearly separated (e.g. by edge position) so ML is needed

## Slide 34: Test case 1 – classification of oxidation states
Oxidation state was determined from integrated spin around Ni absorbing atom
Train error
Test error
Notes: Can you put DUM, RIDGE… at the top
No values in cell

## Slide 35: Test case 2 – regression of average bond length
In both test cases, CDF features can achieve comparable performance as compared to baseline intensity
Tree-based ML algorithms outperform others, consistent with previous works[1-3]
[1] Zheng, C., Chen, C., Chen, Y., & Ong, S. P. (2020) Patterns, 1(2), 100013.
[2] Torrisi, S. B., Carbone, M. R., Rohr, B. A., Montoya, J. H., Ha, Y., Yano, J., ... & Hung, L. (2020). npj Computational Materials, 6(1), 1-11.
[3] Kozyr, E. G., Bugaev, A. L., Guda, S. A., Guda, A. A., Lomachenko, K. A., Janssens, K., ... & Soldatov, A. V. (2021). The Journal of Physical Chemistry C, 125(50), 27844-27852.
For a Ni in octahedron environment, the average bond length is the mean of 6 Ni-O bonds

## Slide 36
Performed linear combination of computational spectra to mimic the site-averaged nature of experimental spectra
Prediction based on CDF feature delivers qualitative agreement with theory
(b)
(a)
Experimental data from Advanced Photon Source, Argonne National Laboratory (US)
Training dataset: Site-averaged spectra for NMC622(~170)
Experimental Ni K-edge XANES  Ni Oxidation state
Yiming Chen et al, “Robust Machine Learning Inference from X‑ray Absorption Near
Edge Spectra through Featurization,” Chemistry of Materials 36, 2304 (2024)

## Slide 37: Experimental Ni K-edge XANES  Ni-O bond length
Prediction based on CDF feature also delivers qualitative agreement with EXAFS analysis
Inhui Hwang and Chengjun Sun
NMC 622
Ni K-edge
Yiming Chen et al, “Robust Machine Learning Inference from X‑ray Absorption Near
Edge Spectra through Featurization,” Chemistry of Materials 36, 2304 (2024)

## Slide 38: Is this CDF thing a fluke? Look at soft x-ray
Trained on simulated O K-edge and Ni L3-edge
Inference based on experimental soft x-ray spectra (Wanli Yang, Gyheok Lee)
CDF gives more reasonable Li content
Lithium content
Voltage (V)
Haili Jia

## Slide 39: Does having multiple edges help?
Experimental values are bulk averages inferred from total current that passed through the system.
Haili Jia

## Slide 40: Oxygen vacancies from multimodal spectra
DFT simulated oxygen vacancy defect structures with different NMC ratio and Li contents
Train ML model (XGBoost) to determine oxygen vacancy from O K-edge and TM L-edge spectra (EELS with spatial resolution)
Co is more sensitive to oxygen vacancies than Ni
Multimodal approach significant boosts the performance
Pristine
5% Oxygen vacancy
Haili Jia
Oxygen vacancy prediction
Mn
Ni
Co
O
All

## Slide 41: FANTASTX – structures from theory + (multimodal) experiments
Have: characterization data; Want: nanoscale atomistic structure
Scope: X-ray, electron microscopy, scanning probe
Challenge: non-unique mapping, underconstrained space
Approach: use physics (Hamiltonian) to constrain solutions
FANTASTX – Fully Automated Nanoscale To Atomistic Structure from Theory and eXperiment
Chaitanya Kolluru
Davis Unruh
Zisheng Zhang
Former: Spencer Hills, Eric Schwenker, Fatih Sen
Notes: To facilitate the interpretation of multimodal data, we are developing a computational framework Fully-Automated Nanoscale To Atomistic Structure from Theory and eXperiment (FANTASTX) which combines atomistic level modeling with an AI engine which samples configurational space and performs pattern matching. Density functional theory (DFT) and force field (FF) calculations allow high-throughput generation of realistic models of atomic arrangements in and out of equilibrium to perform the sampling of possibilities; various approaches are used to accurately compute corresponding scattering, microscopic, and spectroscopic signals. Machine learning, especially pattern recognition and multi-objective supervised learning, is then used to sift through possibilities and determine match to experimental signals, and propose new, related solutions. The result will be a powerful machinery that allows real-time interpretation of materials properties and processes from experiments performed at the CNM and elsewhere.

## Slide 42
Energies
  S/TEM
  XRD/PDF/XR
  XAS/EELS
Match to experiments
  GNN based generative models
  Genetic algorithms
  Basin hopping
  Monte Carlo
Iterative sampling
  DFT
  Interatomic potentials
Computer vision image comparison
Potential parameters fit to DFT data
FANTASTX
Fully Automated Nanoscale To Atomistic Structure from Theory & eXperiment

## Slide 43: FANTASTX in action – STEM
Simulated image
Original image
Robert Klie, Jinglong Guo (UIC)
Eric Schwenker

## Slide 44: XRD: lonsdaleite silicon & rutile titania
Zisheng Zhang

## Slide 45: Pair distribution function: Iridium oxide
Davis Unruh

## Slide 46: XANES: Iron Tris-Bipyridine
[Fe(Dipy)3]2+
Fragments: pyridine rings with varying hydrogenation
Davis Unruh

## Slide 47
“From Data to Wisdom”

## Slide 48: Gathering microscopy & spectroscopy data
EXSCLAIM! EXtraction, Separation, and Caption-based natural Language Annotation of IMages from scientific literature
Problem: lack of microscopy images data (limited small databases)
Scope: any data presented in figures
Challenge: figure separation, caption distribution
Approach: neural networks for figure separation and classification, natural language processing for caption distribution
E. Schwenker, W Jiang, T Spreadbury, O Cossairt, MKY Chan, “EXSCLAIM!--An automated pipeline for the construction of labeled materials imaging datasets from literature” arXiv:2103.10631, Patterns, 2023
Eric Schwenker, Trevor Spreadbury, Weixin Jiang
Weixin Jiang, et al “A Two-stage Framework for Compound Figure Separation,” 2021 IEEE International Conference on Image Processing (ICIP)

## Slide 49: Image and text embeddings
Query = ‘Absorption Spectra'
Output:
Katerina Vriza
Notes: We can observe three main regions in the images: spectral images, molecular structure image and TEM/SEM film images. Maybe add these classes to the text embeddings. Maybe have two different plots for image and text embeddings and show similar areas with the text tags.

## Slide 50: Automated digitization of spectra
Weixin Jiang, E. Schwenker, T Spreadbury, K Li, O Cossairt, MKY Chan, “Plot2Spectra: an Automatic Spectra Extraction Tool,” Digital Discovery 2022.
Weixin Jiang

## Slide 51: Application towards electrochromic polymers
Extract molecular information
Digitize absorption spectra
Set transformer
Random Forest
XGBoost
Absolute error on L*a*b*
KNN
GPR
Lasso
ANN
Train models
Katerina Vriza, Henry Chan, Jie Xu
Autonomous synthesis
Create new materials

## Slide 52: MaterialEyes
https://github.com/MaterialEyes
Software tools
exsclaim – collect images from literature (Trevor Spreadbury, Eric Schwenker, Weixin Jiang)
fantastx – determine nanoscale structures from theory and experiments (Chaitanya Kolluru, Spencer Hills, Eric Schwenker)
ingrained – match simulated & experimental TEM/STM images (Eric Schwenker, Chaitanya Kolluru)
manipulatt – manipulate lattice structures (Joydeep Munshi)
Dataset
atomagined – Simulated STEM dataset (Eric Schwenker) https://doi.org/10.18126/szeq-yde5

## Slide 53
postdoc + internship positions available! (mchan@anl.gov)
Theory+Data-driven approaches  x-ray spectroscopy analysis/acquisition
- Computational spectroscopy explains features
- Manifold projection image segmentation enables robust phase recognition in XANES mapping
- Recursive feature elimination accelerates data capture using fewer energy points
- Comprehensive featurization tests show cumulative distribution function to be superior
- Multimodal: our greatest hope?

## Slide 54: Acknowledgements
Funding
Center for Nanoscale Materials
DOE Early Career award
Data/AI/ML at SUF grants (4DCamera, AIMM, Digital Twin)
Center for Electrochemical Energy Science, a DOE Energy Frontier Research Center (EFRC)
Laboratory Directed Research and Development (LDRD) funding from Argonne National Laboratory
DOE EERE SunShot BRIDGE and PVRD programs
NSF MRSEC
Computational resources
CNM Carbon Cluster
National Energy Research Scientific Computing Center (NERSC)
Laboratory Computing Resource Center (LCRC) at Argonne National Laboratory
Joint Laboratory for System Evaluation (JLSE) at Argonne National Laboratory.
This talk has been created by UChicago Argonne, LLC, Operator of Argonne National Laboratory ("Argonne"). Argonne, a U.S. Department of Energy Office of Science laboratory, is operated under Contract No. DE-AC02-06CH11357. The U.S. Government retains for itself, and others acting on its behalf, a paid-up, nonexclusive, irrevocable worldwide license in said article to reproduce, prepare derivative works, distribute copies to the public, and perform publicly and display publicly, by or on behalf of the Government.

## Slide 55: The DOE Nanoscale Science Research Centers: User Facilities for Creating, Characterizing, and Understanding Nanomaterials
About the Center for Nanoscale Materials:
Free access to staff expertise and equipment (if intent is to publish)
Three annual proposal calls; short-term projects are accepted continuously
Simple 2-page proposal
Co-located with Advanced Photon Source and Argonne Leadership Computing Facility
Center for Nanoscale Materials Capabilities:
Synthesis – 2D materials, biofunctional structures, diamond/CNT, colloidal chemistry, self-assembly, quantum and energy materials
Nanofabrication – 11,000 sq. ft. cleanroom, direct-write fabrication, nonlinear phenomena, nanoscale interaction manipulation, device integration, NEMS/MEMS, flat lens optics
Advanced Microscopy – synchrotron hard x-ray nanoprobe, ptychography, AFM/STM (LT, SP, UHV, optical, synchrotron x-ray), aberration-corrected and in-situ TEM/STEM
Nanophotonics – ultrafast transient absorption and emission spectroscopy and microscopy; UV-to-THz
Theory/Modeling – electronic structure calculations, atomistic studies, electrodynamics, multiscale approaches, machine learning
mchan@anl.gov

## Slide 56
THank You for your attention

## Slide 57
postdoc + internship positions available! (mchan@anl.gov)
Theory+Data-driven approaches  x-ray spectroscopy analysis/acquisition
- Computational spectroscopy explains features
- Manifold projection image segmentation enables robust phase recognition in XANES mapping
- Recursive feature elimination accelerates data capture using fewer energy points
- Comprehensive featurization tests show cumulative distribution function to be superior
- Multimodal: our greatest hope?