## Slide 1
Phonon-mediated High-voltage Detector with Background Discrimination
Rupak Mahapatra
Texas A&M
0


## Slide 2: Low-mass Dark Matter and Reactor CENS Detection Synergy
Both experiments need low-threshold (sub-keV), large-mass detectors
Background (mostly electron recoil) becomes a major hurdle for discovery
Reactor CENS Rate @MINER
Recoil threshold in eV

## Slide 3: SuperCDMS iZIP and HV Detector Technologies
iZIP Detector with ionization and phonon sensors for Electron Recoil (ER) and Nuclear Recoil (NR) discrimination to ~keVnr scale. Low voltage (~3V) operation. Threshold dominated by ionization noise and reduced ionization yield (Lindhard) at low Energy
https://arxiv.org/pdf/1610.00006.pdf
High Voltage : Phonon signal dominated by NTL phonons. Thus, we lose the independent primary phonon measurement. High Voltage Detector with no discrimination, but low threshold of ~100 eVnr.
Trick to overcome Lindhard: convert ionization to phonon
First SNOLAB Si HV (fabricated at TAMU)
First SNOLAB Ge iZIP (fabricated at TAMU)
Phonon
Ionization

## Slide 4: MIER Experiment
Top View
Precisely Movable Core to Probe m-scale Oscillation
Key Features
Low-threshold (<100 eV) with sensitivity to CNS
2-10 m proximity to core (rate enhancement)
Moveable Core tests short baseline oscillation
CNS sensitivity in a few months
Detect CENS and use it to probe BSM Physics, including sterile-
Apply technology to Reactor Monitoring

## Slide 5: Need low threshold or background rejection? Expected Backgrounds in High Voltage Detectors
32Si and 3H limiting backgrounds
  β-decay in detector bulk
  3H produced cosmogenically in Ge and Si, builds up over time (τ = 12.3y )
  32Si produced cosmogenically from argon in atmosphere, seeps into natural Si and ends up in crystals
  Some control by limiting surface exposure of components and detectors
Si
Ge
After Analysis
Selection
3He + 32Si
Ge Activation
Surface Betas
Surface 206Pb
Neutrons
CNS
Demonstrating low threshold (100 eV NR) with ER/NR discrimination is extremely challenging, but has huge benefits for dark matter searches and CNS measurements

## Slide 6: Dedicated Fab @ TAMU 1st SNOLAB Tower Completed!
Polish
Deposition
Photo Coat
Circuit Mask Exposure
Chemical Etch
Multi-step process repeatable for high quality detectors
XRD
Inspect and Package

## Slide 7: Hybrid HV Detector Principle
Charge transport from LV region to HV almost 100%
55Fe
241Am
Main idea: Monolithic detector with a low voltage (LV) and high voltage (HV) sides: LV to measure primary phonons like ZIP and HV to measure NTL phonons. Minimize HV to LV NTL phonon pollution using geometric suppression at the neck
ΔV ~ Large
ΔV ~ Small
0
Holes
e-
Phonons
e-
NTL Phonons
Geometry Simulation with COMSOL Multiphysics

## Slide 8: Hybrid HV Detector Principle
Charge transport from LV region to HV almost 100%
55Fe
241Am
Main idea: Monolithic detector with a low voltage (LV) and high voltage (HV) sides: LV to measure primary phonons like ZIP and HV to measure NTL phonons. Minimize HV to LV NTL phonon pollution using geometric suppression at the neck
Geometry Simulation with COMSOL Multiphysics
0
Holes
e-
Recoil Phonons
e-
NTL Phonons

## Slide 9
Main idea: Detector with a low voltage (LV) and high voltage (HV) sides:
LV to measure primary phonons like ZIP HV to measure NTL phonons.
Minimize HV to LV NTL phonon pollution
Add up phonon signal expected in HV and LV sides
HV
LV
Simulated bands for events in the LV fiducial region with measured resolutions and Lindhard
Parameters:
VHV = 9.6 V
VLV = 2.4 V
ηHL= 0.46
ηLH= 0.10
σLV = 215 eV
𝜖eh~ 4 eV
L in literature
ηHL, ηLH : phonon leakage fractions HV to LV and vice-versa
VHV and VLV are the estimated biased voltage across the detector
L: Lindhard factor, 𝜖eh : Average energy to create e-h pairs in Si
Hybrid HV Detector Principle

## Slide 10: Detector Testing: Charge Transport and Phonon Collection
Fabricated detector
1” HV CDMS mask on top side
3” HV phonon sensor CDMS mask on bottom side
PCB electrode for charge study
Individual QET

## Slide 11: Charge Transport Study
One of the first concerns was how well the charge would be drifted from the LV region to the HV region. Uncollected charge will lead to low yield NR like events
We used contact free electrodes (see next talk by Nader) to study the charge collection and field shaping issues before proceeding with the phonon sensor fab
11
241Am (60 keV) source is taped to the bottom electrode (outer edge of Qi), inside a
collimator with estimated rate of 1.25 Hz
Charge readout using CDMS electronics and a CAEN digitizer

## Slide 12
12
Spectrum from 241Am with biased Voltage: +100V
2D distribution of events in outer electrode vs inner electrode
60 keV events (green dots) are distributed equally between the two electrodes due to large mean free path while the lower energy x-rays (14, 26 keV, red dots) are concentrated on inner electrode.
Hybrid Detector: Results from various runs
Charge Transport Study

## Slide 13
13
Phonon channel layout in the hybrid detector
Externally QET Bias
Figure 1: External Biasing scheme for top phonon channel
Figure 2: Standard Biasing scheme for bottom phonon channels
Phonon Transport Hybrid Detector: Results from various runs
Hybrid Detector: Results from various runs
Phonon Transport Study

## Slide 14
14
Distribution of events at 0V between top and bottom side
Hybrid Detector: Results from various runs
Phonon Transport Study
241Am
Based on the amplitudes of the 60 keV events in the two regions, the various
parameters of our model are calculated.
55Fe
The VHV parameter is estimated from distribution
of events at 12V biased voltage using the equation
VHV, calculated = 9.7 V V HV, estimated = 8 V
Simulated Voltage drop

## Slide 15
15
Hybrid Detector: Results from various runs
NTL Gain Linearity
15
The NTL Linearity of the 5.9 keV events on the (a) top side and the 60 keV events on the (b) bottom side of the detector is verified. Phonon baseline resolution(resolution of detector for 0 keV events) is found to improve with increase in voltage bias.
(a)
(b)
Figure: Phonon baseline resolution as a function of voltage
Figure: NTL gain with voltage
(a)
(b)
Top
Bottom
NTL:

## Slide 16: Phonon only detector with ER/NR Discrimination
A high-statistics dataset of 252Cf neutron source is used to define the electron recoil
and nuclear recoil bands in the yield vs energy plot.
https://inspirehep.net/literature/1802528
Discrimination improves at low energies. Funded by DOE to push the DM and CENS discovery potential – background is key to discovery
Funded by DOE Detector R&D funding since 2017
Ongoing work:
Position correction as done in SuperCDMS
Field shaping to minimize low field regions
Ge hybrid
Narrower neck
Higher bias voltage and discrimination study
NR calibration

## Slide 17: Reactor CENS: Ionization/Light Quenching Requires Stringent Detector Performance
Light (quenched) | Ionization (quenched) | Phonon(no quenching)
Lindhard=.1-.2 | .15 (Ge), .05 (Si) | No Quenching!
Need Eth =20 eV | 30eV(Ge),10(Si) | 100 eV(Ge),300 eV(Si)
Need =4 eV | 5 eV (Ge), 2 (Si) | 40 eV
CRESST (10 gm) | CDMS(kg), CONNIE(gm) | CRESST, CDMS (kg)
Lindhard (1/7 – 1/50 in ROI) kills the ionization/light
Need low thresholds of few eVee and large mass
Leading technologies with discrimination (SuperCDMS, CRESST, Xenon) give up discrimination or give up mass
Challenge is to reduce and reject background, while maintaining threshold and reasonable payload mass
H
phonons
ionization
Q
L
scintillation
eV, =~10%
10s eV, =~1-10%
meV, =~100%
Si
Ionization Efficiency
Nuclear Recoil Energy
Threshold and discrimination dramatically enhance detection. MIER had recent breakthroughs in both
MW Reactor
Scale for Power and 1/r2

## Slide 18: Dark Matter and CENS– Game Changing Technologies in Hand!
10-kg 100-ev NR Ge Hybrid (discrimination gives 10-DRU)
1 day for 5- detection
10-kg 100-ev NR Si Hybrid (discrimination gives 10-DRU
10 days for 5- detection
Exposure in kg-days
10-kg 100-ev NR Si HV (without discrim. 100-DRU)
100 days for 5- detection
10-kg Non-Phonon (Lindhard) detector (1000-DRU without discrimination and without background modeling) – Integrate on tails
1000-10000 days for 5- detection
MW Reactor
Scale for Power and 1/r2
Reactor CENS experiments will not only help us understand fundamental new physics, but also fundamentally change how we use the unstoppable neutrinos to detect threat!