## Slide 2: Multilayer particles
LbL capsules: applications
  Sustained release
  Targeted drug delivery
  Dual drug delivery
  Sensor/detector
B. Koppolu, M. Rahimi, S. Nattama, A. Wadajkar, and K. Truong Nguyen, Development of multiple-layer polymeric particles for targeted and controlled drug delivery, Nanomedicine: Nanotechnology, Biology and Medicine, 6, 355-361
W. Xu, P.A. Ledin, F.A. Plamper, C.V. Synatschke, A.H.E. Müller, and V.V. Tsukruk, Multiresponsive Microcapsules Based on Multilayer Assembly of Star Polyelectrolytes, Macromolecules 2014, 47, 22, 7858–7868
O. Kreft, A. Muñoz Javier, G.B. Sukhorukovac and W.J. Parak, Polymer microcapsules as mobile local pH-sensors, J. Mater. Chem., 2007,17, 4471-4476
PLGA Shell
Hydrophobic drug
Hydrophilic drug
Magnetic core
NIPAAM
Notes: NIPAAM : N-isopropylacrylamide
PSS - PDMAEMA : Poly(sodium 4-StyreneSulfonate) - Poly(2-(dimethylamino)ethyl methacrylate)
pH detector: SNARF-1-dextran conjugate

## Slide 3
A. de Hemptinne
W. De Malsche
µFlow group
Chemical engineering
Vrije Universiteit Brussel
Microfluidic device for multicoating of magnetic microparticles
Notes: a

## Slide 4: Layer-by-Layer reaction (LbL)
2X
Polyacrylic acid 0.033 % (PAA)
Polyethyleneimine 0.033 % (PEI)
In bulk

## Slide 5: Layer-by-Layer reaction (LbL)
AQ. Alorabi, MD. Tarn, J. Gómez-Pastora, E. Bringas, I. Ortiz, V.N. Paunov and N. Pamme, On-chip polyelectrolyte coating onto magnetic droplets – towards continuous flow assembly of drug delivery capsules, Lab Chip, 2017,17, 3785-3795

## Slide 6: Diffusion – calculation
  If 0.5 mm wide streams: contact between reactants after 5.5 minutes
  Polymer cross 10% of central stream (0.05 mm) in
    16 s for PAA
    11 s for PEI
  PAA in ethanol: CD=7.9*10-11 m²/s
  PEI in ethanol: CD=1.1*10-10 m²/s

## Slide 7: Diffusion – measure
Diffusion of fluorescein in water
  CD=5.79*10-10 m²/s, 0.05 mm
    Theoretical diffusion time = 2.15 s
    Experimental diffusion time = 1.5 s
  Need to avoid diffusion for LbL on chip
  Add walls
Chart: 0,69s
Chart: 0,09s
Chart: 2,79s
(a)
(b)
(c)
(d)
(e)
(f)

## Slide 8: Microfluidic chip with hindered diffusion
0.5 mm channels

## Slide 9: Microfluidic chip with hindered diffusion
10 mm
Magnet
Flow focusing
Outlet
Bridges 5 and 6

## Slide 10: Hydraulic resistance theory
Adapt position of the walls to balance the pressure between the bridges
i
j
k
Ohm’s law

## Slide 11: Hydraulic resistance theory
i
j
k
i | 0.56 mm
j | 0.47 mm
k | 0.38 mm

## Slide 12: Microfluidic chip with hindered diffusion
10 mm
Magnet
i | 0.56 mm
j | 0.47 mm
k | 0.38 mm
i | 0.5 mm
j | 0.5 mm
k | 0.5 mm

## Slide 13: Microfluidic chip with hindered diffusion

## Slide 14: Microfluidic chip with hindered diffusion
Polyacrylic acid 0.033% (PAA) Polyethyleneimine 0.033% (PEI)

## Slide 15: On chip LbL
No magnets, no layer
(a)
Four magnets, two layers
(b)
Eight magnets, four layers
(c)
Dipping time of 2,9 s

## Slide 16: On chip LbL
Chart: Fluorescence
| No Layer | PAA/PEI_Rh | PAA/PEI_Rh/PAA/PEI_Rh
 | 287.2218 | 384.3238 | 490.3537

## Slide 17: Conclusions
Device for continuous multicoating of magnetic particles
  Open chamber
  Walls to minimize the diffusion
  Optimize chip geometry
Evaluate the chip by coating of particles
Main assets:
  reducing of dipping time
  automatization of the LbL coating

## Slide 18: Magnetic field-based chip for LbL coating
Future perspective
  Increase the number of layers
  Create particles with specific properties with the use of dedicated LbL reactant

## Slide 19: Thank you
A. de Hemptinne, P. Gelin, I. Ziemecka, W. De Malsche. Microfluidic device for multilayer coating of magnetic microparticles, Submitted in Powder Technology, September 2022

## Slide 20: Hydraulic resistance theory
HENRIK BRUUS. Theoretical Microfluidic.; 2008.
Ohm’s law

## Slide 21: Hydraulic resistance theory
Tanyeri M, Ranka M, Sittipolkul N, Schroeder CM. A microfluidic-based hydrodynamic trap: Design and implementation. Lab Chip. 2011;11(10):1786-1794.
HENRIK BRUUS. Theoretical Microfluidic.; 2008.